## Slide 1: LP30 solution NMR
09-05-2024
LP30 in a plastic tube inserted into a J-young NMR tube with DMSO for locking.

## Slide 2: 1H LP30
O1p= 3.884 ppm

## Slide 3: 31P LP30
O1p= -144 ppm

## Slide 4: 19F LP30
O1p= -74.74 ppm

## Slide 5: PF6 in EC:PC +H2O solution NMR
09-05-2024
By Pablo- for manuscript reviewer comments
in a plastic tube inserted into a J-young NMR tube with DMSO for locking.

## Slide 6: 19F
LP30

## Slide 7
LP30

## Slide 8: 31P

## Slide 9: LP30 solution NMR benchtop
10-04-2024
LP30 in a plastic tube inserted into a J-young NMR tube with DMSO for locking.- same sample that was used for high resolution

## Slide 10: 1H LP30
O1p= 3.884 ppm

## Slide 11: Solution NMR HF, Li/Na/K salts (Cam)
June 2023

## Slide 12: 19F Solution NMR: Effects of HF Acid Addition on H2O and LP30
Addition of approximatly 0.5 mM of HF acid to H2O and LP30 (±5 mL)
The sample was transferred to a plastic capillary and placed within a j-Young’s capillary along with DMSO-d6 for locking purposes.

## Slide 13: Addition of 0.3 mg glass fiber separator
HF
-158 ppm
LiBF4
-150 ppm
LiBF4
-156 ppm
HF
-190 ppm

## Slide 14: HF solution

## Slide 15: Cam’s samples

## Slide 16: Li/Na/K salts

## Slide 20: T1 relaxation summary
 | Salt | HF
Li | 2.30.06 | 10.4; 0.020.02
Na | 2.20.06 | 1.270.7 ; 0.040.05
K | 2.60.08 | No HF signal
 | Salt | HF
Li |  | 
Na |  | 
K |  | No HF signal